## Slide 1: Nanoimprinting technology
Molecular imprinting nanotechnologies has attracted considerable research interest in that nanostructured MIPs (N-MIPs) show significantly improved characteristics in contrast to bulk MIPs
N-MIPs have higher surface area-to-volume ratios, providing a good accessibility to target species and leading to the improvement of binding kinetics and binding capacity.
The templates located within x-nm from the surface can be removed from the bulk materials with a scale of d, and the resultant effective volume of imprinted materials that can rebind target species is
In general, the x value is very small for bulk materials.
When the imprinted materials with the same size were prepared in the form of nanostructures with a scale of 2x nm, all of the templates can be completely removed from the highly crosslinked matrix, and the resultant sites are all effective for target species.

## Slide 2: Nanoimprinting technology
Thus, nanoimprinted materials are expected to improve the binding capacity, binding kinetics, and site accessibility of imprinted materials N-MIPs with different forms such as nanoparticles, nanotubes and nanowires have been synthesized by using different nanotechnologies
Zhang et al. reported the surface imprinting of 2,4,6-trinitrotoluene (TNT) molecules at the surface of silica nanoparticles.
  The uniform core–shell particles with TNT-imprinted polymer nanoshells had a high density of effective recognition sites, which was nearly 5-fold higher than that of traditional imprinted materials.
  The results provided a new strategy for preparing nanosized imprinted materials.

## Slide 3: Comparison of bulk MIPs and Nanostructured MIPs

## Slide 4
Fig. Schematic representation of nanoimprinting.
(A) Schematic illustration of the distribution of effective binding sites in the imprinted bulk materials
and the nanosized, imprinted particles after the removal of templates.
(B) Schematic diagrams of nanoimprinting process for different forms of N-MIPs. (a) Imprinting on the SiO2 support for the formation of core–shell imprinted nanoparticles. SiO2 core particles were first modified with the vinyl functional monomer, followed by initiating an imprinting polymerization reaction, leading to the formation of imprinted shells at the surface of silica particles.
(b) Imprinting on silica nanotubes for the formation of imprinting nanotubes. SiO2 nanotubes were first modified with APTS, followed by the sol–gel process, leading to the formation of imprinted shells at the surface of SiO2 nanotubes.
(c) Imprinting on a sacrificial membrane support by employing an immobilized protein template approach for the formation of imprinted nanowires. The template molecule was firstly immobilized on the inner wall of a porous alumina membrane, followed by imprinting polymerization reaction, leading to the formation of nanowires by removing supporting alumina.

## Slide 5: Special imprinting
Some special imprinting strategies have emerged, such as multi-template imprinting, multi-functional monomer imprinting, dummy imprinting and segment imprinting strategies
Fig. representation of special imprinting. (A) Schematic diagram of multiple template imprinting for multi-analyte binding. (B) Schematic diagram of
multiple functional monomers imprinting for Pb+2

## Slide 6: Special imprinting
(C) Schematic diagram of dummy imprinting. Using trinitrophenol (TNP) as the dummy template for determination of 2,4,6-trinitrotoluene (TNT) based on the fact that TNT has a similar structure as TNP. (D) Schematic diagram of
fragment imprinting. Using part of target molecular as the template, recognition sites were created by the removal of the template molecule, the
obtained recognition sites can bind the whole target molecule based on the fact that target molecule has a fragment structure like the template
molecule

## Slide 7
Fig. 11 Schemes of stimuli responsive MIPs. SR-MIPs are divided into two main types: single responsive MIPs and dual/multi responsive MIPs. Single
responsive MIPs mainly include magnetic responsive using Fe3O4 as response unit, thermo-responsive using N-isopropylacrylamide (NIPAAm) as
response unit; photo-responsive using azobenzene as response unit and pH responsive MIPs using poly(acrylic
acid) as response unit; etc. Dual/multi responsive MIPs mainly include magnetic/thermo responsive MIPs using
Fe3O4 and NIPAAm as response units, photo/thermo responsive MIPs using azobenzene and NIPAAm as response
units; thermo/pH responsive MIPs using NIPAAm and 4-vinylphenylboronic acid (p-VPBA) as response units; thermo/photo/pH responsive MIPs using
azobenzene, NIPAAm and 4-((4-methacryloyloxy)-phenylazo)benzoic acid (MPABA) as response units.
Stimuli responsive MIPs.

## Slide 8
Sample pre-treatment: (selective sorbent materials)
Especially for trace/ultra trace level analytes, samples should be enriched or transformed into optimal forms prior to the final instrument analysis.
Choosing the appropriate sample pre-treatment techniques plays an important role in qualitative and quantitative determination.
  Liquid liquid extraction (LLE) is the most widely used pre-treatment technique while it has the disadvantages of large organic solvent consumption and low enrichment efficiency.
  In order to overcome those drawbacks, a series of extraction techniques have been developed, such as liquid phase microextraction (LPME), solid phase extraction (SPE), solid phase microextraction (SPME) and stir bar sorption extraction (SBSE).
However, these extraction, lack selectivity and suffer from matrix interferences
Fortunately, MIPs have outstanding recognition performances towards target template molecules, and therefore they can be utilized as selective sorbent materials in the customized pretreatment techniques.
Applications of MIPs

## Slide 9
Chromatographic separation:
MIPs are also used as stationary phases in chromatography techniques, such as HPLC, capillary electrochromatography (CEC), capillary LC (CLC) and thin layer chromatography (TLC), as packing materials and monolithic column materials, due to their high affinity and selectivity to the target analytes.
Chemical and biological sensing
The employment of MIPs as specific sensing materials in sensors, namely MIP-based sensors, which were first proposed by Mosbach to monitor the specific binding of vitamin K1 to a ‘‘surface-imprinted’’ silicon surface by using optical surface ellipsometry, has made considerable progress due to their high selectivity and stability, simplicity, cost-effectiveness, and versatility in the fields such as clinical diagnostics, environmental control, food analysis and drug screening.
The characteristic feature of MIP-based sensors is that the MIPs have both recognition and transduction properties, that is, the MIPs as recognition elements can specifically bind target analytes and as transduction elements can generate output signals for detection.
.
Applications of MIPs

## Slide 10: Applications of MIPs
Fig. Structural diagram of the applications of MIPs in pre-treatment techniques, chromatography and sensor. Abbreviations: SPE, solid phase
extraction; DSPE, dispersive SPE; MSPD, matrix solid phase dispersion; SPME, solid phase microextraction; SBSE, stir bar sorption extraction; HPLC, high
performance liquid chromatography; CEC, capillary electrochromatography; CLC, capillary liquid chromatography.

## Slide 11: Applications of MIPs
Figure: Schematic representation of the preparation of antibody-binding-site mimics. Theophylline, the print molecule, binds effectively to the imprint sites, whereas the structurally closely related caffeine does not.
Imprints against the bronchodilator drug theophylline and against the tranquillizer diazepam have shown astonishingly specific recognition
In fact, when these MIPs were tested in competitive radioimmuno- style assays, their recognition of related structures was either nonexistent or far below that of the original print molecule.
Amazingly, the cross-reactivity profiles of these MIPs was practically identical to those reported for monoclonal antibodies against these drugs.
The anti-theophylline MIPs were used for the determination of theophylline concentrations in patient serum samples, pointing towards their use as stable alternatives to antibodies

## Slide 12: Protein imprinting
Fig: Highly schematic presentation of the concept utilized in a protein imprinting protocol. After allowing the protein to interact with functional monomers, the protein is 'surface
imprinted' to a carrier. Subsequent protein recognition is specific for the print protein,
owing to the complementary binding sites.
the specific binding of the glycoprotein transferrin on imprints obtained by surface imprinting

## Slide 13
Thank You!!