## Slide 1: Polymer Nanocontainers (Contd.) : Layer by Layer (LbL) Deposition
Polyelectrolyte self-assembly at charged surfaces to produce polymer capsules.
By use of layer-by-layer (LbL) deposition steps of oppositely charged polyelectrolytes.
The driving force behind the LbL method at each step of the assembly is the electrostatic attraction between the added polymer and the surface.
Polyelectrolyte molecules having the opposite charge (e. g., polycations) are readily adsorbed due to electrostatic interactions with the surface.

## Slide 2: Layer by Layer (LbL) Deposition
All of the ionic groups of the adsorbed polyelectrolyte are not consumed by the electrostatic interactions.
The original surface charge is usually overcompensated by the adsorbed polymer.
Thus the surface charge of the coated particle changes its sign.
Which is further available for the adsorption of a polyelectrolyte of again opposite charge (i. e., a polyanion).

## Slide 3
Preparing hollow spheres using layer-by-layer deposition of oppositely charged polyelectrolytes on colloidal particles and subsequent encapsulation of polymers in a “ship in a bottle” fashion. PSS: sodium polystyrene sulfonate; PAH: poly(allylamine) hydrochloride.

## Slide 4: Layer by Layer (LbL) Deposition
Particles with diameters ranging from 0.2 to 10 mm has been reported.
Thickness of the layered shell is determined by the number of polyelectrolyte layers.
A variety of charged substances, such as synthetic polyelectrolytes, biopolymers, lipids, and inorganic particles have been incorporated as layer constituents.
As a template for this approach, mainly colloids
Polystyrene latexes or melamine formaldehyde particles, gold and proteins have been used as templates

## Slide 5: Layer by Layer (LbL) Deposition
Biopolymers like alginate and polylysine can also be used in a similar way to yield biocompatible nanocapsules.
Uncharged hydrophobic compounds could be also encapsulated using the LbL technique.
Core formed by uncharged low molecular-weight microcrystalline substances (pyrene and fluorescein diacetate).
dispersed in water via micellization with amphiphilic substances such as ionic surfactants, phospholipids, or amphiphilic polyelectrolytes.

## Slide 6: Layer by Layer (LbL) Deposition
A LbL procedure of depositing layers of polyelectrolytes rendered stabilized core shell particles.
The release of the encapsulated substances followed by the intrinsic fluorescence of the core forming material, was triggered by the addition of ethanol.
Wang et al. designed biologically active polymer microcontainers using the LBL assembly.
They functionalized luminescent polymer containers with anti-immunoglobulin G which rendered them biospecific via their IgG partners.

## Slide 7: Layer by Layer (LbL) Deposition
These quantum dot-tagged beads open new opportunities in a range of biotechnological applications.
quantum dots exhibit higher photo-bleaching threshold, quantum yield, and chemical stability than their organic fluorophore analogs.
their spectral properties can be fine-tuned by controlling their size and, similar to planar LbL luminescent films.
crosslinked luminescent core-shell particles and hollow capsules could also be used as light-emitting devices.

## Slide 8: Layer by Layer (LbL) Deposition
use in the area of biosensing.
The concept of artificial cells has been also applied to polyelectrolyte microcapsules.
Tiourina et al. used hollow microcapsules fabricated by stepwise adsorption of polyelectrolytes and phospholipids as so-called artificial cells.
Showed high permeability for ions.
ion-channel-forming peptides such as gramicidin and valinomycin were incorporated into the lipid–polymer composite shell of the microcapsules resulting in membrane potential comparable to biological cells

## Slide 9: Block Copolymer Self-Assembly
Amphiphilic block copolymers (which are polymers consisting of at least two chemically different parts, hydrophobic versus hydrophilic or rod versus coil) may self-assemble into various lyotropic mesophases (liquid-crystalline mesophases) .
Potential for encapsulating large quantities of guest molecules within their central cavity.
Block copolymer chemistry allows the introduction of a wide variety of different block structures.
Considerably more stable due to their larger size, slower dynamics, and inherent steric stabilization.

## Slide 10: Block Copolymer Self-Assembly
Depending on their block length ratio, the critical aggregation concentration (c. a. c.) of these polymers can be shifted to extremely low values.
Which makes superstructures resistant against dilution – an essential requirement for medical applications

## Slide 11: Shell Cross-linked Knedel’s (SCKs)
Special type of nanoparticles having core-shell morphology.
These systems are formed by aggregation of amphiphilic di- and triblock copolymers into micelles.
An intra micellar crosslinking of the corona-forming blocks leads to the highly stable so-called SCKs, with sizes ranging from 50 to 250 nm.
In a second step, the backbone of the core forming blocks can be cleaved.

## Slide 12: Shell Cross-linked Knedel’s (SCKs)
The low molar-mass degradation products extracted.
Leaving behind nanocages formed by a crosslinked polymer shell.

## Slide 13
General procedure for the
preparation of hollow shell cross-linked
knedels (SCKs) nanocages from amphiphilic
Di block copolymers. poly (e-caprolactone)-block-poly(acrylic acid)-block-poly(acrylamide)

## Slide 14: Block Copolymer Nanocontainers
micelles formed from amphiphilic di- or triblock copolymers for the solubilization of hydrophobic drugs.
In aqueous solution, the hydrophobic blocks form the micellar core while the hydrophilic ones build the corona.
The core serves as a microenvironment for the lipophilic drugs, while the outer shell serves as a stabilizing interface between the hydrophobic core and the external medium.
Example 1 : Meier’s group has described the spontaneous formation of vesicles resulting from the self-assembly of a poly(2-methyloxazoline)-block-poly(dimethylsiloxane)- block-poly(2-methyloxazoline) (PMOXA-PDMS-PMOXA) triblock copolymer

## Slide 15: Block Copolymer Nanocontainers
polymer was additionally modified with reactive methacrylate groups at the ends of the hydrophilic blocks.
shape-persistent polymer nanocontainers were formed due to free radical polymerization of these methacrylate end groups.
diameters ranging from 50 to 250 nm.
Example 2: amphiphilic ABC triblock copolymers, with two different water-soluble blocks A and C (A = poly(2-methyl oxazoline), PMOXA; B = poly(dimethyl siloxane), PDMS; C = polyethylene oxide, PEO).

## Slide 16: Block Copolymer Nanocontainers
Similar nanospheres with superior properties inherent to the asymmetry of their membrane were obtained.
Extremely high mechanical stability with high flexibility provided by the hydrophobic PDMS middle blocks.