## Slide 1: Block Copolymer Protein Hybrid Systems (Polymer nanocontainer with controlled permeability)
A new type of hybrid material emerged from the combination of biological molecules and block copolymers.
A new class of biologically “active” super-amphiphiles composed of a block copolymer and an enzyme was designed.
Consisting of an enzyme head group and a single covalently connected hydrophobic polymeric tail.
Obtained by the coupling of maleimide-functionalized polystyrene to a reduced lipase.

## Slide 2: Block Copolymer Protein Hybrid Systems
lipase remained functional in the self-assembled superstructures of these ‘Super amphiphiles’.
A pH-sensitive hybrid material produced by the formation of polymer vesicles or “peptosomes” by the self-assembly of poly(butadiene)-block-poly(L-glutamate) in dilute aqueous solution.
Poly(L-glutamate) performs a pH-dependent helix-coil transition that does not alter the vesicle morphology.
Due to their hydrophilic polypeptide chains, copolymer vesicles seemed to be particularly suited for biological applications.

## Slide 3
(a)Schematic view of a ABA triblock copolymer vesicle and magnification of the structure of its membrane, showing the constituting polymer chains.
(b) Representation of a BioNanoreactor with encapsulated b-lactamase and inserted membrane channel proteins to facilitate diffusion of substrates and products in and out of the nanoreactor.

## Slide 4
(c) Model of viral DNA encapsulation via phage binding and injection into nanocontainers, and transmission electron micrograph (TEM) showing the binding of a phage onto an ABA triblock copolymer vesicle.

## Slide 5
(d) Schematic representation of an ABA nanocontainer with incorporated ionophores in its membrane used as biomineralization device. TEMs showing
(e) calcium phosphate crystals after 1 h and
(f) after 24 h.

## Slide 6: Block Copolymer Protein Hybrid Systems
Membrane receptors can also be incorporated into the walls of such polymer nanocontainers.
access to the proteins could be controlled to a certain degree via the length of the hydrophilic blocks of the underlying amphiphilic block copolymers.
longer hydrophilic chains, they are “hidden” below a hydrophilic polymer layer so that larger ligands had no access to them.
Such receptors bearing channels provide as an elegant method to load polymer nanocontainers with DNA.

## Slide 7: Block Copolymer Protein Hybrid Systems
The electroneutrality and the low immunogenicity and toxicity of such DNA-loaded nanocontainers renders them highly interesting as new vectors for gene therapy.
Receptor-bearing polymer nanocontainers may be of particular interest as biosensors.
Major advantage of these systems is that an entire detection and signaling cascade can be incorporated into a single nanocontainer.
Block copolymer nanocontainers can be regarded as miniaturized artificial cells allowing for massive miniaturization.

## Slide 8: Block Copolymer Protein Hybrid Systems
high mechanical and(bio)chemical stability, the polymer containers provide a constant environment for encapsulated analytic molecules
Hypothetical representation of a cell-like structure in which DNA is transcribed to RNA and translated to the protein via an encapsulated transcription and translation systems.

## Slide 9: Stimuli-responsive Nanocapsules
Stimuli-responsive peptides and proteins incorporated into the walls of polymer nanocontainers can be used as “switches” to control molecular exchange across polymer membranes.
Such systems can be regarded as mimetics of virion cages, which show a structural transition that leads to the opening of gated pores within the virus shell upon pH changes.
Can be obtained by core-shell emulsion polymerization.
A two-step polymerization led to crosslinked poly(acrylic acid) hollow spheres that undergo a pH-induced swelling transition.

## Slide 10: Stimuli-responsive Nanocapsules
The carboxylic acid groups of the polymer particles of the systems dissociate increasingly with the rise in pH.
Generating a high negative charge density along the polymer backbone .
These containers can retain encapsulated material at low pH and released it in “one shot” at high pH.
Example : pH-responsive microparticles have been proposed for the oral delivery of insulin.
The insulin-containing particles retain the substance at low pH in the stomach until they reach a higher pH in the intestine.

## Slide 11: Stimuli-responsive Nanocapsules
Delivery system consists of insulin-containing microparticles of crosslinked copolymers of poly(methacrylic acid)-graft-poly(ethylene glycol).
Reversible formation of interpolymer complexes stabilized by hydrogen bonding between the carboxylic acid protons and the ether groups on the grafted chains led for pH sensitivity.

## Slide 12: Nanoparticle Films
The formation of nanoparticle layers on a solid support in a “bottom up” approach.
These thin films are formed by surface-modified nanoparticles.
The attractive electrostatic interactions between charged nanoparticles and functionalized surfaces are frequently exploited.
variations in the pH of a solution can be used to control the degree of ionization of the particle surfaces.

## Slide 13: Nanoparticle Films
Modulation of the electrostatic interactions between nanoparticles and the immobilizing surface.
Examples:
a) Dendrimers : The large number of end groups at the periphery of a dendrimer and the relative ease of their tailoring leads to a plethora of pathways for surface recognition.
b) SCKs: surface-functionalized to promote cell binding via conjugation between the SCK nanoparticles and a biologically active peptide sequence.

## Slide 14: Biomaterials and Gene Therapy
Field of biomaterials focuses on the design of “intelligent” materials.
that is, it can respond to their surrounding environment to improve their integration and function.
Example: polymer nanoreactors can be used for the incorporation and controlled release of polypeptide growth factors that are inherent to biological function regulation (e. g., tissue regeneration).
An alternative approach to viral gene delivery: complexation of DNA with cationic lipids, polycationic polymers, and dendrimers

## Slide 15: Biomaterials and Gene Therapy
Both liposomes and biocompatible block copolymer nanocontainers can be used.
enables the genetic material to be protected against the action of endonucleases.
due to their limited blood clearance and drainage into the lymphatic system (in case of tissue injection).
Further, block copolymer chemistry would allow the preparation of nanocontainers with the potential to encapsulate large quantities of guest molecules within their central cavity,

## Slide 16
Model mechanism of DNA transfection using active dendrimer mediated
uptake.

## Slide 17: Outlook
The principle of combining the high diversity of polymer chemistry with the functionality of natural proteins and peptides will have many future applications in areas such as :
drug delivery,
sensor technology,
energy conversion,
diagnostics,
catalysis.

## Slide 18: Outlook
The possibility of incorporating biological functions into these synthetic structures.
The possibility of incorporating additional design criteria (e. g., temperature sensitivity, targeting moieties, special surface characteristics) makes polymer nanocontainers highly versatile systems.