## Slide 1: Luminescent Quantum Dots for Biological Labeling
BBL 747
Bionanotechnology

## Slide 2: Overview
The integration of nanotechnology with biology and medicine is expected to produce major advances in medical diagnostics, therapeutics, molecular biology, and bioengineering
Recent advances have led to the development of functional nanoparticles (electronic, optical, magnetic, or structural) that are covalently linked to biological molecules such as peptides, proteins, and nucleic acids
Due to their size-dependent properties and dimensional similarities to biomacromolecules, these bioconjugates are well suited as contrast agents for in-vivo magnetic resonance imaging (MRI), as nanoscale carriers for drug delivery, and as nanostructured coatings and scaffolds for medical implants and tissue engineering
In comparison with organic dyes and fluorescent proteins, semi-conductor quantum dots (QDs) represent a new class of fluorescent labels with unique advantages and applications.
For example, the fluorescence emission spectra of QDs can be continuously tuned by changing the particle size, and a single wavelength can be used for simultaneous excitation of all different-sized QDs

## Slide 3: Quantum Dots
Quantum dots (QDs), often described as ‘artificial atoms,’ exhibit discrete energy levels, and their bandgap (distance between the valance band of electrons and conduction band) can be precisely modulated by varying the size .
QDs are nanometer-scale semiconductor crystals composed of groups II to VI or III to V elements and are defined as particles with physical dimensions smaller than the exciton Bohr radius
QDs exhibit unique luminescence characteristics and electronic properties such as wide and continuous absorption spectra, narrow emission spectra, and high light stability .
They absorb white light and then re-emit a specific color a few nanoseconds later depending on the bandgap of the material .

## Slide 4
Figure: Ten distinguishable emission colors of ZnS-capped CdSe quantum dots excited with a near-
UV lamp. From left to right (blue to red), the emission maxima are located at 443, 473, 481, 500, 518, 543,
565, 587, 610, and 655 nm.

## Slide 5: Preparation of QDs
Surface-passivated QDs are highly stable against photobleaching and have narrow, symmetric emission peaks (25–30 nm full width at half maximum).
It has been estimated that CdSe quantum dots are about 20 times brighter and 100 times more stable than single rhodamine 6G molecules
Semiconductor QDs (e. g., CdSe, CdTe, CdS, ZnSe, InP, and InAs) are most often composed of atoms from groups I–VII, II–VI, or III–V elements.
Earlier attempts to synthesize QDs were conducted in aqueous environments with stabilizing agents such as thioglycerol and polyphosphate.
However, the resulting QDs showed poor quantum yields (<10 %) and broad size distributions (relative standard deviation RSD > 15 %). Quantum yield is a ratio of the number of photons emitted to the number of photons absorbed.
A high-temperature organometallic procedure for QD synthesis yields near-perfect nanocrystals with quantum yields as high as 50% at room temperature, and a particle size distribution as narrow as 5 %.

## Slide 6: Preparation of QDs
To prepare type II–VI QDs, a metal precursor (such as dimethyl cadmium) and a chalcogenide compound (such as selenium) were first dissolved in tri-n-butyl phosphine (TBP) or tri-n-octyl phosphine (TOP), and are then injected into a hot coordinating solvent such as tri-n-octylphosphine oxide (TOPO) at 340–360 °C.
Studies conducted, have shown that high-quality nanocrystals could also be prepared by using CdO as an inexpensive starting material
The nanocrystal size can be tuned by heating QDs in TOPO at 300 °C for an extended period of time (ranging from seconds to days, depending on the desired particle size), in which the QDs grow by Ostwald ripening.
In this process, smaller nanocrystals are broken down, and the dissolved atoms are transferred to larger nanocrystals.
The rate of growth is dependent upon temperature and the amount of limiting reagents.
Alternately, continuous injection of organometal/chalcogenide precursors at 300 °C can be used to increase the size of QDs

## Slide 7: Passivation of QDs
For improved optical properties, the QDs are often coated and passivated by a thin layer of a higher bandgap material. For example, the fluorescence quantum yields of CdSe QDs increase from 5% to 50% with one to two monolayers of ZnS capping
At present, ZnS and CdS are most commonly used to cap CdSe QDs. The bandgap energy of bulk CdS is about 0.9 eV higher than that of CdSe, while the ZnS and CdSe bond lengths are similar; these conditions lead to the epitaxial growth of a smooth ZnS layer on the surface of CdSe core particles. Similar procedures have been used to synthesize group III–V nanocrystals such as InP and InAs
Epitaxy refers to the deposition of an overlayer on a crystalline substrate.
Semiconductor QDs absorb photons when the energy of excitation exceeds the bandgap energy. During this process, electrons are promoted from the valence band to the conduction band.
Measurements of UV-Visible spectra reveal a large number of energy states in QDs. The lowest excited energy state is shown by the first observable peak (also known as the quantum-confinement peak), at a shorter wavelength than the fluorescence emission peak.

## Slide 8
Figure: Comparison of the excitation
(top) and emission (bottom) profiles
between rhodamine 6G and CdSe quantum
dots.

## Slide 9: Overview
Excitation at shorter wavelengths is possible because multiple electronic states are present at higher energy levels. In fact, the molar extinction coefficient gradually increases toward shorter wavelengths. This is an important feature for biological applications because it allows simultaneous excitation of multicolor QDs with a single light source.
Light emission arises from the recombination of mobile or trapped charge carriers. The emission from mobile carriers is called “excitonic fluorescence”, and is observed as a sharp peak.
The emission spectra of single ZnS-capped CdSe QDs are as narrow as 13 nm (full width at half maximum or FWHM) at room temperature
Defect states in the crystal interior or on its surface can trap the mobile charge carriers (electrons or holes), leading to a broad emission peak that is red-shifted from the excitonic peak.
Nanocrystals with a large number of trap states generally have low quantum yields, but surface capping or passivation can remove these defect sites and improve the fluorescence quantum yields.
The excitonic fluorescence is dependent on the nanocrystal size. It has been demonstrated that an approximately linear relationship between the particle size and the bandgap energy

## Slide 10: Overview
This quantum–size effect is similar to that observed for a “particle in a box.” Outside of the box, the potential energy is considered to be infinitely high. Thus, mobile carriers (similar to the particle) are confined within the dimensions of the nanocrystal (similar to the box) with discrete wavefunctions and energy levels. As the physical dimensions of the box become smaller, the bandgap energy becomes higher.
For CdSe nanocrystals, the sizes of 2.5 nm and 5.5 nm correspond to fluorescence emission at 500 nm and 620 nm, respectively.
In addition to size, the emission wavelength can be varied by changing the semiconductor material. For example, InP and InAs QDs usually emit in the far-red and near-infrared, while CdS and ZnSe dots often emit in the blue or near-UV
Also, elongated QDs (called quantum rods) show linearly polarized emission, whereas the fluorescence emission from spherical CdSe dots is either circularly polarized or not polarized
In comparison to organic dyes such as rhodamine 6G and fluorescein, CdSe nanocrystals show similar or slightly lower quantum yields at room temperature. The lower quantum yields of nanocrystals are compensated by their larger absorption cross-sections and much reduced photobleaching rates.