## Slide 1: Overview
It was estimated that molar extinction coefficients of CdSe QDs are about 105 to 106 M–1 cm–1, depending on the particle size and the excitation wavelength. These values are 10- to 100-fold larger than those of organic dyes, but are similar to the absorption cross-sections of phycoerytherin, a multi-chromophore fluorescent protein.
It has been estimated that single ZnS capped CdSe QDs are ~ 20 times brighter than single rhodamine 6G molecules. Similarly, phycoerytherin is estimated to be 20 times brighter than fluorescein
Another attractive feature of using QDs as biological labels is their high photostability. The photobleaching rate of silica-coated ZnS-capped CdSe QDs was examined against that of rhodamine 6G.
The QD emission stayed constant for 4 hours, while rhodamine 6G was photobleached after only 10 minutes.
It has been suggested that capped CdSe nanocrystals are 100- to 200-fold more stable than organic dyes and fluorescent proteins. Under intense UV excitation, single phycoerytherin molecules are found to photobleach after 70 seconds, while the fluorescence emission of quantum dots remain unchanged after 600 seconds
The photobleaching of QDs arise from a slow process of photo-induced chemical decomposition. Henglein and coworkers speculated that CdS decomposition is initiated by the formation of S or SH radicals upon optical excitation. These radicals can react with O2 from the air to form a SO2 complex, resulting in slow particle degradation.

## Slide 2: Overview
Single QDs have been shown to emit photons in an intermittent on-off fashion, similar to a “blinking” behavior reported for single fluorescent dye molecules, proteins, polymers, and metal nanoparticles.
The fluorescence of single QDs turns on and off at a rate that is dependent on the excitation power. This phenomenon has been suggested to arise from a light-induced process involving photoionization and slow charge neutralization of the nanocrystals
When two or more electron-hole pairs are generated in a single nanocrystal, the energy released from the combination of one pair could be transferred to the remaining carriers, one of which is preferentially ejected into the surrounding matrix.
Subsequent photogenerated electron-hole pairs transfer their energy to the resident, unpaired carrier, leading to nonradiative decay and dark periods.
The luminescence is restored only when the ejected carrier returns to neutralize the particle.
Thermal trapping of electrons and holes is also believed to be a contributing factor because a dependence of the blinking rate on temperature was observed.
A further finding is that single dots exhibit random fluctuations in the emission wavelength (spectral wandering) over time. This effect is attributed to interactions between excitons with optically induced surface changes

## Slide 3: Biological Applications of QDs
In order to exploit the novel optical properties of QDs for biological applications, a number of methods have been reported for converting hydrophobic QDs to water-soluble and biocompatible nanocrystals
In one approach, mercaptopropyl trimethoxysilane (MPTMS) adsorbs onto the QD surface, and displaces the surface-bound tri-n-octylphosphine oxide (TOPO) molecules.
A silica-shell is formed on the surface by introduction of a base and then hydrolysis of the MPTMS silanol groups. The polymerized silanol groups help stabilize nanocrystals against flocculation, and render the QDs soluble in intermediate polar solvents such as methanol and dimethylsulfoxide.
Further reaction of bifunctional methoxy molecules, such as aminopropyltrimethoxysilane and trimethoxysilyl propyl urea, makes the QDs more polar and soluble in aqueous solution.
In another method, bifunctional molecules such as mercaptoacetic acid and dithiothreitol are directly adsorbed onto the QD surface. Mercapto compounds and organic bases are added to TOPO-QDs dissolved in organic solvents. The base deprotonates the mercapto functional group and carboxylic acid (in the case of mercaptoacetic acid), which leads to a favorable electrostatic binding between negatively charged thiols and the positively charged metal atoms.

## Slide 4: Methods
The QDs precipitate out of solution and can be redissolved in aqueous solution (pH 5). The presence of highly polar functional groups, such as –COOH, –OH, or –SO3Na (from bifunctional mercapto molecules) makes the nanocrystals soluble in water.
A third approach for linking biomolecules onto the particle’s surface is to use an exchange reaction,
in which mercapto-coated QDs are mixed with thiolated biomolecules (such as oligonucleotides and proteins).
After overnight incubation at room temperature, a chemical equilibrium is reached between the thiolated molecules in solution and on the QD surface. This method has been used to adsorb oligonucleotides and biotinylated proteins onto the surface of QDs
Further improved the surface chemistry using a synthetic biopolymer coating.
For example, the water-soluble QDs can be stabilized with a positively charged polymer or a layer of chemically denatured bovine serum albumin (BSA).
A key finding is that the polymer coating restores the optical properties of QDs nearly to that of the original QDs in chloroform. The polymer layer also provides functional groups (amines and carboxylic acids) for covalent conjugation with a variety of biological molecules.

## Slide 5: Methods
A similar approach, in which engineered proteins with a linear positively-charged peptide are directly adsorbed onto negatively charge nanocrystals through electrostatic interactions
Most recently, Wu and coworkers used an amine-modified polyacrylic acid polymer to coat the surface of QDs. The modified polymer was no longer soluble in water, and strongly adsorbed onto TOPO-capped QDs via hydrophobic interactions in chloroform. An important feature of this procedure is that QDs are solubilized without removing the surface ligands (TOPO), which maintains the optical properties of QDs in an aqueous environment.
Similarly, Bubertret et al. encapsulated hydrophobic QDs in small micelles and demonstrated their use in in-vivo cellular imaging. QDs have been used for multiplexed optical encoding and high-throughput analysis of genes and proteins

## Slide 6: Methods
Polystyrene beads are embedded with multicolor CdSe QDs at various color and intensity combinations. The use of six colors and ten intensity levels can theoretically encode one million protein or nucleic acid sequences. Specific capturing molecules such as peptides, proteins, and oligonucleotides are covalently linked to the beads and are encoded by the bead’s spectroscopic signature. A single light source is sufficient for reading all the QD-encoded beads.
To determine whether an unknown analyte is captured or not, conventional assay methodologies (similar to direct or sandwich immunoassay) can be applied. This so-called “bar-coding technology” can be used for gene profiling and high-throughput drug and disease screening.
Based on different principles, Natan and coworkers reported a metallic nanobarcoding technology for multiplexed bioassays.
Together with QD-encoded beads, these “barcoding” technologies offer significant advantages over planar chip devices (e. g., improved binding kinetics and dynamic range), and are likely to find use in various biotechnological applications.

## Slide 7
Figure: Schematic illustration of surface modification methods for linking quantum dots to biomolecules.

## Slide 8
Figure : Fluorescence micrograph of a mixture of CdSe/ZnS QD-tagged beads emitting single-color
signals at 484, 508, 547, 575, and 611 nm. The beads were spread and immobilized on a polylysine-coated
glass slide, which caused a slight clustering effect.

## Slide 9: Outlook
A number of biological labeling applications have been demonstrated for QDs, including DNA hybridization, immunoassays, and receptor-mediated endocytosis.
In particular, multicolor quantum dots are well-suited for the simultaneous labeling of multiple antigens on the surface of normal and diseased cells.
The high photostability of QDs allows not only real-time monitoring or tracking of intracellular processes over long periods of time, but also quantitative measurements of fluorescent intensity.
They allow target detection at the single-copy level, and provide detailed structure information of biological specimens.
Far-red and near-infrared QDs are well-suited for applications in in-vivo molecular imaging and ultrasensitive biomarker detection.
Visible light has been used for cellular imaging and tissue diagnosis, but optical imaging of deeper tissues (millimeters) requires the use of far-red or near-infrared light in the spectral range of 650–900 nm. This wavelength range provides a “clear” window for in-vivo optical imaging because it is separated from the major absorption peaks of blood and water

## Slide 10
Figure : Schematic illustration of cell staining using biomolecules attached with multicolor QDs.
Small color particles represent bioconjugated quantum dots.

## Slide 11
Figure: Immunofluorescence images of human breast tumor cells (BT-474) stained with organic dye (fluoroscein isothiocyanate; FITC) and green quantum dots. Within only 20 seconds of illumination, the organic dye was almost completely photobleached (top panel), while the QD fluorescence image was stable

## Slide 12: Outlook
Under photon-limited in-vivo conditions (where light intensities are severely attenuated by scattering and absorption), the large absorption coefficients of QDs (on the order of 106 cm–1M–1, which is 10–100 times larger than those of common organic dyes) will be essential for efficient probe excitation.
Unlike current single-color molecular imaging, multi-wavelength optical imaging with QDs will allow intensity ratioing, spatial colocalization, and quantitative target measurements at single metastasized tumor sites and for single anatomical structures.
With an inert layer of surface coating, the nanocrystals are less toxic than organic dyes

## Slide 13: Outlook
In preliminary studies, luminescent QDs were conjugated to transferrin (an iron-transport protein), to antibodies that recognize cancer biomarkers, and to folic acid (a small vitamin molecule which is recognized by many cancer cells).
In each case, it was found that receptor-mediated endocytosis occurred and the nanocrystals were transported into the cell. Single QDs as well as clusters of dots trapped in vesicles were clearly visible inside living cells.
In conclusion, semiconductor QDs have been developed as a new class of biological labels with unique advantages and applications that are not possible with organic dyes or fluorescent proteins.
When conjugated with fully functional biomolecules such as peptides, protein, and oligonucleotides, this class of fluorescent tags is well-suited for ultrasensitive imaging and detection.
It is envisioned that the design and construction of multifunctional QDs will allow molecular imaging and diagnostics of single diseased cells.