## Slide 1: S-Layers as Templates for the Formation of Regularly Arranged Nanoparticles
The reproducible formation of nanoparticle arrays in large scale with predefined lattice spacing and symmetries remains a challenge in the development of future generations of molecular electronic devices
Biomolecular templating has proven to be very attractive, as the self-assembly of molecules into monomolecular arrays is an intrinsic property of many biological molecules and has already grown into a scientific and engineering discipline.
The first approach in using S-layers as templates in the generation of perfectly ordered nanoparticle arrays was developed by Douglas and coworkers
  S-layer fragments of Sulfolobus acidocaldarius were deposited on a smooth carbon surface and metal coated by evaporation of a ~ 1 nm-thick tantalum/tungsten film.
  Then, this protein–metal heterostructure was ion milled, leading to 15 nm-sized holes hexagonally arranged according to the center-to-center spacing of the S-layer of 22 nm.

## Slide 2
Structure
Figure: (a) Freeze-etching preparation of whole cells of Thermoanaerobacter thermohydrosulfuricus L111-69 revealing a hexagonally ordered array. Scale bar = 100nm. (b) Three-dimensional model of the S-layer of Bacillus stearothermophilus NRS 2004/3a/V2 exhibiting oblique lattice symmetry. The protein meshwork shows one square shaped, two elongated, and four small pores per morphological unit. (c) Computer image reconstruction of scanning force microscopic images of the topography of the square S-layer lattice from Bacillus sphaericus CCM 2177. The images were taken under water. The surface corrugation corresponding to a gray scale tram black to white is 1.8 nm. Scale bars in (b) and (c) = 10 nm. (d) Schematic drawing of the different S-layer lattice types. The regular arrays exhibit either oblique (p1, p2), square (p4), or hexagonal lattice symmetry (p3, p6). The morphological units are composed of one, two, three, four, or six identical subunits. (Reproduced from Ref. [3], with permission from Wiley-VCH.)

## Slide 3: S-Layers as Templates for the Formation of Regularly Arranged Nanoparticles
The approach was further optimized using S-layer on a smooth graphite surface and titanium oxide for the metal coating
After oxidation in air and fast-atom beam milling at normal incidence, a thin ~ 3.5 nm metallic nano-porous mask with pores of 10 nm.
The same group used low-energy electron-enhanced etching to pattern the surface properties of a silicon substrate through the regularly arranged pores of the S-layer
After etching and removal of the S-layer, the patterned surface was oxidized in an oxygen plasma, leading to a nanometric array of etched holes (18 nm diameter) which served as nucleation sites in the formation of an ordered array of nanometric titanium metal clusters.
In a similar approach using argon ion etching, the S-layer of Deinococcus radiodurans was used as a nanometric template for patterning ferromagnetic films
Uniform hexagonal patterns of 10 nm-wide dots and lattice spacing of 18 nm were fabricated from 2.5 nm-thick sputter-coated Co, FeCo, Fe, FeNi, and NiFe films.

## Slide 4: S-Layers as Templates for the Formation of Regularly Arranged Nanoparticles
A synthesis pathway for fabrication of nanoparticles by wet chemical processes and S-layers as nanometric templates was developed
Self-assembled S-layer were exposed to a metal–salt solution (e. g., [AuCl4]–, [PtCl4]2–), followed by slow reaction with reducing agent such as hydrogen sulfide (H2S).
Nanoparticle superlattices were formed according to the lattice spacing and symmetry of the underlying S-layer.
Since the precipitation of the metals was confined to pores of S-layer, nanoparticles also resembled morphology of pores
The first example exploiting this technique was the precipitation of cadmium sulfide (CdS ) on S-layer lattices composed of SbsB and SbpA
  After incubation of the S-layer self-assembly products with a CdCl2 solution for several hours, the hydrated samples were exposed towards H2S for one or two days.
  The generated CdS nanoparticles were 4–5 nm in size, and their superlattice resembled the oblique lattice symmetry of SbsB (a = 9.4 nm, b = 7.4 nm, g = 80"), or the square lattice symmetry of SbpA (a = b = 13.1 nm, g = 90"), respectively.

## Slide 5: S-Layers as Templates for the Formation of Regularly Arranged Nanoparticles
In a similar approach, a superlattice of 4–5 nm-sized gold particles was formed by using SbpA (with previously induced thiol groups) as a template for precipitation of a tetrachloroauric (III) acid solution(Figure).
Gold nanoparticles formed either by reduction of the metal salt with H2S or under the electron beam in a transmission electron microscope.
The latter approach is technologically important as it allows those areas where nanoparticles are formed to be defined.
As determined by electron diffraction, the gold nanoparticles were crystalline but their ensemble was not crystallographically aligned.
The wet chemical approach was used in the formation of Pd- (salt: PdCl2), Ni- (NiSO4), Pt- (KPtCl6), Pb- (Pb(NO3)2) and Fe- (KFe(CN)6) nanoparticle arrays, and for producing platinum nanoparticles on the S-layer of Sporosarcina ureae

## Slide 6: S-Layers as Templates for the Formation of Regularly Arranged Nanoparticles
Unfortunately, wet chemical methods do not allow varying size or composition of nanoparticles in the fabrication process. Thus, the binding of preformed nanoparticles into regular arrays on S-layers has significant advantages in the development of nanoscale electronic devices
Similar to binding biomolecules (e. g. enzymes or antibodies) onto S-layers, gold or CdSe nanoparticles can be electrostatically bound in regular arrangements on S-layers
The nanoparticles were either negatively charged due to surface citrate ions or positively charged due to surface coating with poly-l-lysine
In summary, these experiments have clearly shown that S-layers are suited to control the formation of nanoparticle arrays, either by direct precipitation from the vapor or liquid phase, or by binding preformed nanoparticles
The S-layer approach provides for the first time a biologically based fabrication technology for self-assembly of molecular electronic or optic devices

## Slide 7
Figure (a) Electron microscopical image of gold nanoparticles (mean diameter 4.5 nm) obtained
using wet chemistry. An S-layer with square lattice symmetry served as template in the precipitation of the metal salt. The gold nanoparticles were formed in the pore region of the protein meshwork under the electron beam. Scale bar = 50 nm.
(b) Electron microscopical image of preformed gold nanoparticles (mean diameter 4 nm) regularly
bound on the surface of an S-layer with square lattice symmetry. Electrostatic interactions between the surface of the nanoparticles and functional domains on the S-layer are responsible for the binding. Scale bar = 100 nm. (Reproduced from Ref. [91], with permission from Elsevier.)

## Slide 8: Conclusion
At present, most applications developed for using S-layers depend on the in vitro self-assembly capabilities of native S-layer proteins in suspension, on the surface of solids (e. g., silicon wafers, metals, polymers), Langmuir-lipid films, and liposomes.
Once the regular arrays have been formed, a broad spectrum of very precise chemical modifications can be applied for tailoring the physico-chemical properties of S-layers and for a defined binding of differently sized functional molecules.
In particular, the possibility of immobilizing or growing other materials (e. g., silicon oxide, metals) on top of recrystallized S-layer lattices with most accurate spatial controlled architecture opens up many new possibilities in nanofabrication and supramolecular engineering
An important line of development for the specific tuning of structural and functional features concerns the genetic manipulation of S-layer proteins.

## Slide 9
Recent studies have clearly demonstrated that truncated S-layer proteins incorporating specific functional domains of other proteins maintain the self-assembly capability into regular arrays
This approach can lead to new iso-porous ultrafiltration membranes, affinity structures, enzyme membranes, ion- and metal particle-selective binding matrices, microcarriers, biosensors, diagnostics, biocompatible surfaces, and vaccines
Moreover, biomimetic approaches copying the supramolecular principle of virus envelopes such as S-layer-coated liposomes will provide new strategies for drug targeting and drug delivery.
Preliminary studies have also provided strong evidence that S-layers have a great potential as patterning elements for non-life science applications (e. g., nonlinear optics and molecular electronics)
Conclusion